Section 08 14 23.19

Part 1	General

  - Section includes non-rated and fire rated wood doors.

- Molded Hardboard Faced Wood Doors

  - Description:

- Section Includes:

  - Wood doors: non-rated and fire doors (20,45,& 60-minute)

- Related Sections:

1.	Section 06 20 00	-	Finish Carpentry

2.	Section 06 40 00	-	Architectural Woodwork

3.	Section 08 11 00	-	Metal Doors and Frames

4.	Section 08 70 00	-	Finish Hardware

5.	Section 09 91 23	-	Interior Painting

  - References

- ANSI/WDMA I.S. 1A -04 Industry Standard for Architectural Wood Flush Doors

- NFPA 80 Standard for Fire Doors and Other Opening Protectives Current Edition

- NFPA252 Standard Methods of Fire Tests of Door Assemblies Current Edition

- UBC STD 7-2 (1997) Fire Tests of Door Assemblies

- UL10C Positive Pressure Fire Tests of Door Assemblies

- NFPA 105 Standard for Installation of Smoke Door Assemblies and Other Openings Protectives (Current Edition)

  - Quality Assurance:

- Meet or exceed WDMA IS-1A 04  “Standard Duty” performance standards

- Positive pressure labeled fire doors: tested and listed in accordance with UL10C, UBC Std 7-2 (1997), NFPA 252

- Installed Door Assembly: Fire rated doors to conform to NFPA 80

  - Warranty:

- Provide manufacturer’s warranty to comply with the following:

- Interior solid core doors; Five year Factory Warranty

- Interior hollow core doors; One year Factory Warranty

- Manufacturer’s warranty excludes the appearance of field-finished door(s).

  - Submittals:

- Submit shop drawings: illustrate and identify door openings to include elevations, sizes, bevels, undercuts, types, fire ratings, swings and machining specifications.

- Submit two samples of painted finish (minimum 8” x 10”) on the specified face material for architectural approval prior to finishing.

- Submit manufacturer’s specification literature to assure product compliance.

- Submit copy of manufacturer’s warranty.

  - Delivery, storage, handling and site conditions:

- Deliver, store, protect and handle doors under provisions of WDMA and manufacturer’s instructions.

- Inspect doors for damage prior to accepting job site delivery

- Do not store doors in areas subject to direct sunlight

- HVAC systems should be operating and balanced prior to the delivery and storage of doors.

  - Relative humidity of not less than 25% nor greater than 55%

E.	Store all doors in horizontal flat position prior to installation

Part 2	Products / Materials

  - Door Types:

- Manufacturer: Lynden Door Standard Series

- Acceptable manufacturers:

  - Lynden Door

  - Algoma

  - Marshfield Door

  - Eggers

- Flush Interior Doors: Typical 1-3/4” unless otherwise noted

  - Door Construction:

- Hollow Core

  - Minimum 1-1/4” (prior to trimming) vertical edges to be solid wood, finger joint stiles are not acceptable.

  - Minimum 2” wood rails

  - Minimum 3” x 6-1/2” lock block at lock stile

  - Additional blocking as required by hardware

- Non-rated and 20-minute rated: Particleboard core 3 ply construction

  - Particleboard LD1 minimum properties

  - Minimum 1-1/4” (prior to trimming) vertical edges to be solid wood, finger joint stiles are not acceptable.

  - Minimum 2” wood rails (When overhead closer is called out in Hardware Schedule minimum rail should be 6”)

- 45, 60 minute fire rated: WDMA FD3 Custom Grade

  - Fire resistant composite core per manufacturer’s label service listing

  - Fabricate in accordance with U.L or Warnock Hersey (ITS) listings.

  - Fire retardant vertical edges compatible with face veneers.

  - Minimum 5” top rail (closer reinforcement)

  - All fire doors designated with surface applied hardware require minimum 400 lbs. screwholding  (reference WDMA P-1 performance standards), reinforce as required.

- 20, 45, and 60 minute fire doors to be supplied as Category ‘B’ construction. See Sectoin 08 70 00 to assure gasketing complies with fire door listing and ‘S’ label requirements

  - Face Material:

- Craftmaster molded panel as indicated on door schedule

  - Factory prefit and undercut for frame openings and dimensions identified on shop drawings and schedules.

  - Factory machine doors for finish hardware in accordance with hardware requirements and dimensions.  Include face holes for mortise and exit devices (excluding trim holes) and thru bolts for lever design cylindrical locks as listed in Hardware Schedule.

  - Factory Finish

A.	Factory painted marr resistant finish per the following:

1.	Color per architect approved sample

2.	 Apply per the following:

a.	Scuff Sand 220 Grit

b.	Primer Interior solvent based lacquer – 4 Wet Mills

c.	Scuff Sand 220 Grit

d.	Paint Interior solvent based lacquer – 4 Wet Mills

e.	Paint Interior solvent based lacquer -  4 Wet Mills (second coat of 				paint only required for darker pigmented paints)

f.	Top Coat	CAB Acrylic Clear Top Coat – 4 Wet Mills with Semi Gloss 				Sheen (40-50 Degrees)

B.	VOC in liquid state not to exceed 617 grams/liter

Part 3	execution

  - Examination

    - Inspect doors for any damage prior to installation.  Do not install damaged doors as installation of damaged doors may void manufacturer’s warranty.

    - Verify frame opening sizes and tolerances are acceptable and ready to receive work.

    - Do not install doors into frame openings which are not plumb and square.

  - Installation

    - Schedule installation of doors after finishing of walls and finish floor installation

    - Coordinate installation of doors with approved Finish Hardware and Frame Schedules

    - Install doors in accordance with ANSI/WDMA IS-1A and NFPA 80 and NFPA 105

    - Do no trim fire doors for width

    - Drill pilot holes for screws

    - Ensure all frames and doors are properly installed level and plumb.

    - Adjust operation of door for smooth and balanced movement.

    - Touch up factory finish and/or repair any damage to doors caused by installation

  - Adjusting

- Adjust operation of door for smooth and balanced movement.

- Do not remove hinge screws after initial insertion.  Shims used for alignment purposes must not be inserted between hinge and the door.

- Doors may be repaired or refinished if work complies with requirements and shows no evidence of repair or refinishing

- Replace doors that are damaged or do not comply with requirements.

  - Protection

    - Protect this work and work of other trades from any damage during installation

  - Cleaning

    - Clean all work installed in this section.  Remove from site all trash, packing material, material scraps and other debris related to the work of this section.

    - Clean doors after installation in accordance with manufacturer’s Care and Handling Instructions

END OF SECTION